## Slide 1
Scanning Probe Microscopy (SPM)
October 2023
SPM User Basic Training
Notes: 10/16/23
1

## Slide 2
Scanning Probe Microscopy (SPM)
History
-1981, Gerd Binnig and H. Rohrer observed electrons tunneling in vacuum
→ Birth of Scanning Tunneling Microscopy (STM)
→ Atomic-scale surface imaging in real space
→ Development of STM
→ New family of microscopy: “Scanning Probe Microscopy (SPM)”
1986 – Nobel Prize to G. Binnig and H. Rohrer.
AFM - Phys. Rev. Letters, 1986, Vol. 56, p 930
- J.Appl.Phys. 1987, Vol. 61, p 4723
Revisitingthe7×7reconstructionofSi(111)
  G. Binnig, H. Rohrer, F. Salvan, Ch. Gerber, A. Baro
  Pages L373-L378
October 2023
SPM User Basic Training
Notes: 10/16/23
2
10/16/23
2

## Slide 3
Scanning Probe Microscopy (SPM)
October 2023
SPM User Basic Training

## Slide 4
Analytical Technique HRS | Signal | Depth Resolution | Lateral Probe Size | Typical application
TXRF Total X-ray Reflection Fluorescence | X-rays |  | 10 nm | Metal contamination
XPS X-ray photoelectron spectroscopy | Photo-electrons | 1-10 nm | 10 μm – 2 mm | Surface analysis depth profile
SEM Scanning electron Microscopy | Secondary & backscattered electrons |  | 3 nm | Surface imaging
AFM Atomic Force Microscopy | Atomic forces | 0,1 nm | 1,5 – 5 nm | Surface imaging
HRSEM High-resolution SEM | Secondary & backscattered electrons |  | 0,7 nm | High resolution surface imaging
STM Scanning Tunneling Microscopy | Tunneling currents | 0,1 nm | 0,1 nm | Surface Imaging
Comparison - Surface Analysis Techniques
October 2023
SPM User Basic Training
Notes: 10/16/23
4
10/16/23
4

## Slide 5
Comparison – SEM/TEM/STM/AFM
October 2023
SPM User Basic Training
Notes: 10/16/23
5

## Slide 6
Scanning Probe Microscopy (SPM)
Basic Principles
→ Raster scanning performed to probe on a surface sample
→ Recording of probe-Sample interaction point-to-point, line-by-line
→ 3-dimensional Map or image of the surface
→ Compared to SEM
→ instead of an electron beam, use of mechanical, opto-mechanical, electrical, magnetic probes
October 2023
SPM User Basic Training
Notes: 10/16/23
6
10/16/23
6

## Slide 7
AFM vs SEM
October 2023
SPM User Basic Training
Notes: 10/16/23
7
10/16/23
7

## Slide 8
AFM vs SEM
October 2023
SPM User Basic Training
Notes: 10/16/23
8
10/16/23
8

## Slide 9
AFM vs SEM
October 2023
SPM User Basic Training
Notes: 10/16/23
9
10/16/23
9

## Slide 10
A Classification of SPM Techniques
October 2023
SPM User Basic Training
Notes: 10/16/23
10
10/16/23
10

## Slide 11
A Classification of SPM Techniques
October 2023
SPM User Basic Training
Notes: 10/16/23
11
10/16/23
11

## Slide 12
Scanning Tunneling Microscopy (STM)
works well only with (electrically) conducting and semi conducting samples.
The STM, a Primary Imaging Mode in SPM, was the first modern SPM, invented in 1982
the probe: sharp metal tip (tungsten, or a platinum-iridium
(Pt-Ir) alloy)
Signal: the tunneling current I between the sample and the tip (typically 100’s pA to several nA) when a bias voltage V (typically 10’s or 100’s mV) is applied between the two.
Surface Studies by Scanning Tunneling Microscopy, Phys. Rev. Lett. 49, 57
Published 5 July 1982, G. Binnig, H. Rohrer, Ch. Gerber, and E. Weibel
Highly oriented pyrolytic graphite
October 2023
SPM User Basic Training
Notes: 10/16/23
12
10/16/23
12

## Slide 13
Magnitude of current I extremely sensitive to V
varying exponentially
  the small gap δ that separates the nearest atoms between the tip and the sample surface.
Scanning Tunneling Microscopy (STM)
October 2023
SPM User Basic Training
Notes: 10/16/23
13
10/16/23
13

## Slide 14
SPM Users Basic Training
August 2010
Scanning Probe Microscopy (SPM)
Atomic Force Microscopy (AFM)
  Contact Mode
  Intermittent Mode (Alternating Contact – AC)
Video
October 2023
SPM User Basic Training
Notes: 10/16/23
14
10/16/23
14

## Slide 15
Atomic Force Microscopy (AFM)
October 2023
SPM User Basic Training
Notes: 10/16/23
15
10/16/23
15

## Slide 16
Atomic Force Microscopy (AFM)
October 2023
SPM User Basic Training
Notes: 10/16/23
16
10/16/23
16

## Slide 17
3 Modes
Contact Mode
Intermittent Mode or Tapping Mode
Non-Contact Mode
Force – distance curve
October 2023
SPM User Basic Training
Notes: 10/16/23
17
10/16/23
17

## Slide 18
Force – distance curve
October 2023
SPM User Basic Training
Notes: 10/16/23
18
10/16/23
18

## Slide 19
Contact Mode
Advantages
  Easy set up
  Fast imaging
  Friction signal
  Force vs. distance measurements
Disadvantages
  Lower resolution due to lateral forces
  Possible tip and/or sample damage from vertical forces.
Mode choice usually dictated by sample.
October 2023
SPM User Basic Training
Notes: 10/16/23
19
10/16/23
19
19

## Slide 20
Contact Mode Feedback Loop
October 2023
SPM User Basic Training
Notes: 10/16/23
20
10/16/23
20
20

## Slide 21
Contact Mode Image Channels (Typical)
Topography: Calibrated voltage sent to Z piezo by feedback loop.
Deflection: Same as Error Signal, equals Deflection minus Setpoint. Shows edges more clearly.
Friction: (A+C) – (B+D) / Sum, measures twisting of cantilever due to frictional effects of sample surface.
October 2023
SPM User Basic Training
Notes: 10/16/23
21
10/16/23
21
21

## Slide 22
Contact Mode Image Channels: Why Monitor Friction?
Topography image of polymer film
Friction - Trace
Friction - Retrace
Friction reveals hidden information about the sample.
All three images acquired simultaneously from same sample area.
Notes: 10/16/23
22
10/16/23
22

## Slide 23
Force curve measurement
October 2023
SPM User Basic Training
Notes: 10/16/23
23
10/16/23
23

## Slide 24
Force curve analyzes can be used to determine chemical and mechanical properties such as adhesion, elasticity, hardness and rupture bond lengths.
The slope of the deflection (C) provides information on the hardness of a sample.
The adhesion (D) provides information on the interaction between the probe and sample surface as the probe is trying to break free. Direct measurements of the interactions between molecules and molecular assemblies can be achieved by functionalizing probes with molecules of interest
Force curve measurement
Link
October 2023
SPM User Basic Training
Notes: 10/16/23
24
10/16/23
24

## Slide 25
October 2023
SPM User Basic Training
Video
October 2023
SPM User Basic Training

## Slide 26: Acoustic AC (AAC) Mode
SPM Users Basic Training
August 2014
Cantilever oscillated near resonance frequency.
Amplitude rather than deflection is feedback loop input.
Uses stiffer cantilevers than contact mode.
October 2023
SPM User Basic Training
Notes: 26
10/16/23
26

## Slide 27
October 2023
SPM User Basic Training

## Slide 28: AAC Mode: Typical Image Types
SPM Users Basic Training
August 2014
→ Topography: Same idea as in contact (calibrated voltage sent to piezo) but oscillation amplitude is feedback loop input, not deflection.
→ Amplitude: Error signal, difference between setpoint amplitude and actual amplitude.
→ Phase: Lag between phase of driving signal and response of cantilever. Very sensitive to material differences in sample and can show details not readily seen in Topography image.
Notes: 28
10/16/23
28

## Slide 29
August 2010
SPM User Basic Training

## Slide 30: AAC Mode: Resonant Frequency Shift During Approach
SPM Users Basic Training
August 2014
Notes: 30
10/16/23
30

## Slide 31
August 2010
SPM User Basic Training

## Slide 32
Phase Imaging of Sample Elasticity
The phase lag changes depending on the mechanical properties of the sample surface
Notes: 10/16/23
32

## Slide 33
Phase Imaging of Sample Elasticity
(a) Non-contact AFM image and (b) phase image of block co-polymers, collected simultaneously. Field of
view 1 μm × 1 μm
Notes: 10/16/23
33

## Slide 34
Conductive AFM
Notes: 10/16/23
34

## Slide 35
The contrast on the Conductive AFM image indicates differences in the electrical property of the raised dots. (Scan Size: 3 μm × 3 μm )
Conductive AFM
Notes: 10/16/23
35

## Slide 36
Electrostatic Force Microscopy (EFM)
EFM maps locally charged domains on the sample surface
Notes: 10/16/23
36

## Slide 37
Electrostatic Force Microscopy (EFM)
Notes: 10/16/23
37

## Slide 38
Lateral Force Microscopy (LFM)
(top) The PSPD of AFM and (bottom) LFM
Notes: 10/16/23
38

## Slide 39
Lateral Force Microscopy (LFM)
(a) Topography and (b) LFM image of human hair. (20 μm scan size)
Notes: 10/16/23
39

## Slide 40
Magnetic Force Microscopy (MFM)
Notes: 10/16/23
40

## Slide 41
Magnetic Force Microscopy (MFM)
Notes: 10/16/23
41

## Slide 42
Magnetic Force Microscopy (MFM)
Notes: 10/16/23
42

## Slide 43
Nanoidentation
Notes: 10/16/23
43

## Slide 44
Pattern created on the surface by plowing the surface with the tip (a) and by changing the surface with applied bias (b).
Nanolithography
Notes: 10/16/23
44

## Slide 45
Applications of AFM
Nano-Surface Texture/Roughness:
Notes: 10/16/23
45

## Slide 46
AFM Analysis of Peptide
Notes: 10/16/23
46

## Slide 47
“The surface of human red blood cells after treatment with an antibiotic peptide"
Dr Luciano Paulino Silva. Embrapa Recursos Genéticos e Biotecnologia (Brazil)
The STM image shows a self-assembled disordered pattern formed by cytosine molecules on a Au(111) surface
"2D organic glass formed by adsorption of cytosine molecules on a Au(111) surface"
Dr. Wei Xu. Interdisciplinary Nanoscience Center (iNANO) (Denmark)
An Escherichia coli cell is imaged using tapping mode AFM under dry condition
"Escherichia coli (E. coli) with Pili and Flagella"
Mr Ang Li. National University of Singapore (Singapore)
http://www.icmm.csic.es/spmage/index.php
AFM Images Gallery
Notes: 10/16/23
47

## Slide 48
AFM Analysis of membrane porosity
Notes: 10/16/23
48

## Slide 49
AFM Analysis of Nanoparticles
Notes: 10/16/23
49

## Slide 50
AFM Analysis of Dentine
Notes: 10/16/23
50

## Slide 51
AFM Analysis of polymer nanofibers
Notes: 10/16/23
51

## Slide 52
AFM images. (a) Condensed mass of brome mosaic virus (BMV), (b) Helical, rod-shaped tobacco mosaic virus (TMV), (c) Tangles of marine filamentous bacteriophage and their broken fragments scattered on the AFM substrate. (d) Virions of Tipula iridescent virus, a very large icosahedral virus that infects insects. The virions of BMV have a diameter of 30 nm, TMV is about 20 nm in diameter and1,000 nm in length, and the adenovirus and iridovirus have diameters of about 100 nm and 200 nm, respectively.
AFM Analysis of Virus
brome mosaic virus
rod-shaped tobacco
mosaic virus
Notes: 10/16/23
52

## Slide 53
AFM Artifacts
Surface features appear too large
Notes: 10/16/23
53

## Slide 54
AFM Artifacts
Notes: 10/16/23
54

## Slide 55
AFM Artifacts
Notes: 10/16/23
55

## Slide 56
AFM Artifacts
Notes: 10/16/23
56

## Slide 57
AFM Artifacts
Notes: 10/16/23
57

## Slide 58
AFM Calibration
Notes: 10/16/23
58

## Slide 59
Notes: 10/16/23
59